Comparative structural analyses of monovalent cation-exchanged birnessite

Seohee Yun

Crystallography Lab

Department of Earth System Sciences, Yonsei University

Birnessite (Na0.54Mn2O4∙1.5H2O), as one of the major constituents in manganese nodules, is a layered manganese oxide mineral. The layer is formed by edge-sharing of MnO6 octahedra, which stacks in ~7 Å spacing where water molecules and Na+ cations are occupied in a loosely disordered fashion. As such, the interlayer cations can be mixed with or substituted by other cations to affect their crystallo-chemical properties as well as to contain diverse rare metals and chemical species. To understand comparative crystal chemistry of birnessite as a function of interlayer cation substitution, a series of monovalent cation-exchanged forms, i.e., H-, Li-, K-, NH4-, Rb-, and Cs-exchanged birnessite, were produced from Na-birnessite under ambient conditions and analyzed using synchrotron X-ray powder diffraction, thermogravimetry, and X-ray photoluminescence spectroscopy. The the interlayer spacing is found to be correlated with the ionic radius of the interlayer cation and water content in an opposite manner, i.e., the (001) spacing generally expands as a function of ionic radius while it contracts as a function of the weight percentage of water molecules. Compared to the original Na-birnessite, ion-exchanged forms show generally higher Mn3+ to Mn4+ ratio, which seems to be correlated to the water content. Using the Rietveld structural refinements, the interlayer structural models are categorized into two groups depending on the distribution of cations and water molecules, i.e., water molecules and cations in the Li-, K-, Rb-, Cs-birnessite models occupy separate interlayer sites whreas those are statistically mixed in the H-, Na-, NH4-birnessite models. The complex interplay among cation type, water content, Mn oxidation state, and structural parameters is discussed to understand the comparative crystal chemistry of birnessite and its potential role on the geochemical cycle of Mn minerals in deep sea environments.